## Slide 1
FUNCTION OF A RELEASE AGENT
Concrete bonds to mould / formwork. Release agents are primarily used to assist in the clean, easy and stripping of a mould / formwork from concrete without damaging the concrete or the mould / formwork and ensure high quality fair faced stain free concrete
Wood
Metal
Plastic + other
Steel / aluminium
plastic, polystyrene, rubber, latex, fibreglass
In order to achieve the satisfactory concrete release from a mould / form, it is imperative to choose the correct release agent.
This comprehensive guide is designed to help you select the right product.
SHUTTERING AND MOULD OIL RELEASE AGENTS
timber, plywood,
resin ply, shutter board
Notes: Slide no.1

## Slide 2
ADVANTAGES OF EASTTO OILS
MOULD / FORM PROTECTION
Easy, clean release of the mould / formwork from concrete; without damaging the mould / formwork or the concrete Protects and extends the life of the formwork / mould.
Reduces the like lihood of imperfections and surface damage (particularly blow holes) to the concrete, creating more durable and attractive concrete surfaces.
AESTHETIC CONCRETE
Does not stain or affect the colour of the concrete.
Does not affect the adhesion of subsequent finishes and coatings. Plaster, paint and other coatings may be applied subsequently.
PRODUCT QUALITY
Does not affect the hydration of concrete.
Eastto Release Agents are safe to use, and avoid hazardous materials regulations in transport and disposal.
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 3
ADVANTAGES OF EASTTO OILS
Have a low odour, and are inoffensive to use.
Ready to use product –far more convenient and reduces the likelihood of errors that can occur if mixing is required.
Storage – our products have one year storage life!
SHUTTERING AND MOULD OIL RELEASE AGENTS

## Slide 4
APPLICATION ADVICE FOR FORMWORK
    Eastto Range prevents the veneer on the shutter boards from delaminating.
  Use Eastto Shuttering Oil / Mould Oil
    Eastto Range contain temporary rust preventive qualities
    Use Eastto Shuttering Oil / Mould WCX
  Any release agent containing a solvent may cause the above material to become brittle or disintegrate.
    Use Eastto S huttering Oil / Mould WCX
Wood
Plastic + others
(timber, plywood,
resin, shutter board) ply
(plastic, polystyrene,
rubber, latex, fibreglass)
Metal
Test panels that are built before construction are the best method for assessing the suitability of a release agent for a given application.
(steel / alumini)
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 5
HOW TO APPLY
  Eastto Oils should be applied before concreting starts and reinforcement is fixed and as near as possible to the first concrete pour and prior to subsequent pours
  Spraying should be shielded as misting in the air may be detrimental to the person spraying and the environment. Use hoods over spray nozzle to prevent misting. (this will prevent clogging of the spray jet and over spray)
  Eastto Oils should be applied in a uniform, continuous film, as thinly as possible. The surface of the mould / form should appear slightly greasy (have a shine). It can be a pplied by brush / Swab / Spraying / Dipping.
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 6
HOW TO APPLY
  Too much is as bad as too little
    Too little – surface damage to concrete and formwork / moulds (surface plucking / mould stick: where patches of the concrete surface stick to the form / mould and are then pulled off the face during formwork / mould removal.
    Too much – blow holes, staining, colour variation, efflorescence, dusting, even retardation of the concrete. Excess oil can also cause ground contamination. Excessive application results in ‘ pooling’. If there is an over application, wipe it off with a clean rag.
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 7
APPLICATION ADVICE FOR POTENTIAL PROBLEMS
Problem | Causes | Remedy
Blow holes | Air entrapment against formwork (usually visible on vertical surfaces due to high surface tension) | Increase vibration, make concrete mix less sticky
Flaking with rough surfaces | When precast units are de - moulded while still green (moisture content is too high) | Increase retention time.
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 8
CONSTRUCTION SITES
CONSTRUCTION SITES |  |  | 
Timber Formwork | Timber & Plastic + others | All types of formwork | 
SHUTTERING OIL / MOULD OIL / MOULD WCX | SHUTTERING OIL / MOULD OIL | SHUTTERING OIL / MOULD OIL | SHUTTERING OIL / MOULD OIL
Any Oil
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 9
CONSTRUCTION SITES
PRECAST |  |  |  | 
Dry |  | Wet |  | 
Steam cured |  | Steam cured |  | Not Steam cured
SHUTTERING OIL | MOULD OIL | SHUTTERING OIL | MOULD WCX | ALL THREE TYPES
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 10
SHUTTERING OIL
  Mineral based
  Suitable to pre - cast
  Used on all types of formwork
  Ideal for formwork suppliers
  Contains no Solvents
  Easy Stripping
  All types of moulds
SUMMARY
Wood
Metal
Man - made
FORMWORK
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 11
MOULD OIL
  Mineral based
  Suitable for steam curing
  Ideal for pre - cast pipes.
SUMMARY
FORMWORK
Wood
Metal
Man - made
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 12
MOULD WCX
  Mineral based
  Suitable for steam curing
  Ideal for pre - cast pipes.
SUMMARY
FORMWORK
Wood
Metal
Man - made
SHUTTERING AND MOULD OIL RELEASE AGENTS
Notes: Slide no.1

## Slide 13
Eastto Range |  |  | 
Eastto Shuttering Oil |  |  | 
Eastto Mould Oil |  |  | 
Eastto Mould WCX |  |  | 
Wood
Metal
Plastic +
others
SHUTTERING AND MOULD OIL RELEASE AGENTS
MOULD WCX

## Slide 14
Eastern Petroleum Private Limited
Regd. Off: Unit No. 1, ‘Riddhi Siddhi’, Coprorate Park, V N Purav Marg,
( Sion Trombay Road ), Chembur, Mumbai - 400 071. MH, India.
Tel: +91 - 22 - 2529990 / 4232 4121,
Fax: +91 - 22 - 4232 4131 / 2524 1895,
Email: office@easternpetroleum.in,
office@eastto.in
Web: www.easternpetroleum.in